Millennium Tiles, LLC	May 2015

550 East Centralia Street

Elkhorn, WI 53121

Phone: 262-723-7778

Fax: 262-723-7629

Website: www.millenniumtiles.com

E-mail: info@millenniumtiles.com

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice.

The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all Specifier Notes when editing this section.

Section numbers and titles are from MasterFormat 1995 Edition, with numbers and titles from MasterFormat 2004 Edition in brackets.  Delete version not required.

Brackets indicate options in text to be filled in or deleted by the author; they should NOT be visible in final document.

SECTION 07 42 13 [07410]

ZALMAG® STEEL WALL TILES

Specifier Notes:  This section covers Millennium Tiles, LLC ZALMAG® STEEL roof/wall tiles.  Consult Millennium Tiles for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Galvanized ZALMAG® steel wall tiles.

1.2	RELATED SECTIONS

Specifier Notes:  Edit the following list of related sections as required for the project.  List other sections with work directly related to this section.

A.	Section 06 10 00 [06100] – Rough Carpentry: Wall sheathing

B.	Section 07 25 00 [07270] – Air and Vapor Barriers

C.	Section 07 62 00 [07620] – Sheet Metal Flashing and Trim.

D.	Section 07 92 00 [07920] – Joint Sealants.

1.3	REFERENCES

Specifier Notes:  List standards referenced in this section, complete with designations and titles.  This article does not require compliance with standards, but is merely a listing of those used.

A. 	ASTM A1046/A1046M – Standard Specification for Steel Sheet, Zinc-Aluminum-Magnesium Alloy-Coated by the Hot-Dip Process, 2014.

B.	ASTM D4479/D4479M – Standard Specifications for Asphalt Roof Coatings – Asbestos-Free; 2000.

C.	ASTM E8/E8M – Standard Test Methods for Tension Testing of Metallic Materials; 2013.

D.	ASTM E18 - Standard Test Methods for Rockwell Hardness of Metallic Materials; 2014.

1.4	SUBMITTALS

A.	See Section 01 33 00 [01330] – Submittal Procedures for additional requirements.

B.	Product Data:  Submit manufacturer’s product data, including surface preparation and installation instructions.

C.	Samples:  Submit two [____] full samples of each color of ZALMAG® steel wall tiles.

D.	Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

E.	Installation Instructions:  Manufacturer’s written instructions including surface preparation and installation procedures

1.5	DELIVERY, STORAGE, AND HANDLING

A.	Delivery:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.	Storage:  Store materials in clean, dry area in accordance with manufacturer’s instructions.

C.	Handling:  Protect materials during handling and installation to prevent damage.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	Millennium Tiles, LLC, 550 East Centralia Street, Elkhorn, WI 53121 Phone 262.723.7778 Fax 262.723.7629 Website www.millenniumtiles.com  E-mail info@millenniumtiles.com

B.	 Substitutions: Not allowed [See Section 01 60 00 [01600] – Product Requirements].

2.2	MATERIALS

A.	ZALMAG® STEEL Roof/Wall Tiles:

1.	Description:  Individual roof/wall tiles with 4-sided interlocking design, self-aligning tab, and concealed nailing strip with 2 holes.

2.	Material:  ZALMAG® STEEL.

a.	Base Material:  ASTM A1046/A1046M, with corrosion-resistant coating.

b.	Coating consists of Zinc, Aluminum, Magnesium and Silicon.

Specifier Notes:  Specify Size & Weight to be used on Project.

3.	Size:

a.	Large Tiles:  15 inches by 9-5/8 inches; Exposure:  14-1/2 inches by 8-5/16 inches +/- 1/16 inch.

b.      T.S. Panel:   7-3/4 inches by 17-1/4 inches; Exposure:  7-1/4 inches by

16-1/4 inches +/- 1/16 inch.

b.	Accent Tiles:  [___] inches by [___] inches; Exposure:  [___] inches by [___] inches.

c.	TS Tiles:  [___] inches by [___] inches; Exposure:  [___] inches by [___] inches.

4.	Weight:

a.	Large Tiles:  0.91 lbs./sq. ft.

b.      T.S. Panel:  0.89 lbs./sq. ft.

b.	Accent Tiles:  [___]./sq. ft.

c.	TS Tiles:  [_____] lbs./sq. ft.

5.	Thickness:  0.015 inch +/- .002 inch (28-gage), mill tolerances apply.

6.	Density:  0.284 lbs./cu. in.

7.	Temper:  Hot Rolled

8.	Tensile Strength:  ASTM E8/E8M, 50,000 psi.

9.	Yield Strength: ASTM E8/E8M, 27,600 psi.

10.	Elongation: ASTM E8/E8/M 22%

11.	Rockwell Hardness: ASTM E18, 58

12.	Thermal Conductivity:  360 BTU-in/hr-ft²-ºF ²-°F

14.	Performance Ratings:

a.	Wind:  110 mph; Miami-Dade County Notification No. ATIWI 07009

b.	Fire:  ULClass A, B, or C.

Specifier Notes:  For Large tiles specify style(s) to be used on Project

- Large Tile Style:

  - Flat Tile

  - Shadow Cup Tile

Specifier Notes: Specify finish of material. Consult Millennium Tiles, LLC for availability of different finishes.

- Finish:

  - Natural

  - Pre-Patina II

Specifier Notes:  Select applicable color(s).

- Color:

  - Natural (no color)

  - Kijani Green

  - Barna Bronze

2.3	ACCESSORIES

A.	Trim and Flashing:  Same material, finish, and gauge as ZALMAG® wall tiles except where otherwise noted; See Section 07 62 00 [07620] - Sheet Metal Trim and Flashing for additional fabrication requirements.

Specifier Notes:  Edit the follow list as required.

1.	False Starter:  1-3/4 by 120 inches; 22 [24]-gage

2.	Inside Corners:  6-1/8 by 6-1/8 by 120 inches; 22 [24]-gage

3.	1-Piece Outside Corners:  120 inches long; 22 [24]-gage

4.	3-Piece Outside Corners:  120 inches long; 22 [24]-gage; consist of 2 J-channels and 1 Outside Corner Cap (2 by 2 inches).

5.	J-Channels:  3-3/8 by 1/2 by 120 inches; 22 [24]-gage

6.	Head Flashing:  1-1/2 by 1-3/4 by 120 inches; 22 [24]-gage

B.	Underlayment:  ASTM D 226/D 226M, No. 30 asphalt-saturated felt.

C.	Air and Water Barrier:  See Section 07 25 00 [07270] – Weather Barriers.

D.	Fasteners:  Galvanized steel, ring-shank roofing nails.

1.	Minimum Length:  3d (1-1/4 inches)

E.	Joint Sealants:  Exterior-grade, high-temperature, silicone joint sealant, as specified in Section 07 92 00 [07920].

F.	Bituminous Paint:  Asphaltic mastic, ASTM D 4479/D 4479M, Type I.

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine substrate to receive ZALMAG® steel wall tiles.

B.	Notify Architect of conditions that would adversely affect installation.

C.	Do not begin surface preparation or installation until unacceptable conditions are corrected.

D.	Ensure wall sheathing is solid with a minimum thickness of:

1.	Plywood:  1/2 inch.

2.	Oriented Strand Board (OSB):  1/2 inch.

E.	Ensure weather barrier in properly installed and undamaged.

3.2	SURFACE PREPARATION

A.	Prepare surfaces in accordance with manufacturer’s instructions.

B.	Ensure surfaces to receive ZALMAG® steel wall tiles are smooth and even, and that there are no protruding nail heads.

Specifier Note:  Delete the following if not used in wall assembly

C.	Install drainage/ventilation mat in accordance with manufacturer’s instructions.

3.3	INSTALLATION

A.	Install ZALMAG® steel wall tiles in accordance with manufacturer’s instructions.

B.	Pull tiles from several boxes during installation process to ensure random color variation.

C.	Use specified fasteners at spacing in accordance with manufacturer’s instructions.

Specifier Note:  Most common source of galvanic action is from zinc to copper.

D.	Prevent Electrolysis:

1.	Prevent dissimilar metals and corrosive nonmetallic materials from coming into direct contact with ZALMAG® steel materials.

2.	Do not allow water to flow from dissimilar metals to ZALMAG® steel materials.

E.		Install trim and flashing in accordance with manufacturer’s instructions.

F.	Joint Sealants:

1.	Install joint sealants as specified in Section 07 92 00 [07920].

2.	Install joint sealants at overlapping flashing and exposed fastener heads.

3.4	PROTECTION

A.	Protect installed ZALMAG® steel wall tiles to ensure that, except for normal weathering, tiles will be without damage or deterioration at time of substantial completion.

END OF SECTION